Lilley Group Experiment/Sample Summary

Gas Tight Samples

Color/Number Identifiers

| GT color | GT # |
| --- | --- |
| Red | 10 |
| Orange | 16 |
| Yellow | 17 |
| Blue | 6 |
| White | 14 |
| Bare | 15 |

Sample List

| GT color | Dive # | Location | Tmax (ºC) |
| --- | --- | --- | --- |
| Blue | 4013 | Hot Harold | 286 |
| Orange | 4013 | Roane | 187 |
| Bare | 4014 | DK1 | 28 |
| White | 4015 | Cuchalain | 307 |
| Red | 4015 | Stonehenge | 302 |
| Blue Major Pair | 4016 | Site of diffuse flow meter | Low T |
| Blue | 4017 | Sully | 363 |
| White | 4018 | Clambed (near RAS intake) | 305 |
| Bare | 4018 | Clambed (diffuse site) | 57 |
| White | 4021 | Hulk | 297 |
| Bare | 4021 | Grotto | 333 |
| Red | 4021 | Milli-Q | 310 |
| White | 4024 | Nootka Cold Seep | Backgrd |
| Blue Major Pair | 4024 | Nootka Cold Seep | Backgrd |

Sensors

The pressure sensor near Homer #91 and Grotto was recovered on dive 4014 and the data successfully downloaded.  The sensor was not re-deployed due to communications difficulties.  We listened to the res probe on dive 4017 and got a temperature reading of 363 ºC, and a resistivity reading of 79 mV which indicates a fluid that is enriched in chloride with respect to seawater. The validity, or lack thereof, of this reading will become more clear once the full record has been retrieved. However, the fact that the temperature reading seemed accurate was enough to justify leaving The res probe deployed for continued data recording.

Materials Test and Pump Test

An apparatus including two titanium tubes to test both a direct siphoning of vent fluid and a pumping of the fluid through a cooling coil were deployed on dive 4017 at Sully.  Attached to the intake of the system were titanium wire cages containing samples of several materials.  The experiment was recovered on dive 2021.  The siphon began to work right away but appeared to stop up at least in the first couple as days as a flyby on 4019 did not show obvious flow.  The pump intake was blocked during deployment and that test was inconclusive.  Of the materials that were tested,  alumina and graphite seemed to fare well.  Boron nitrate disintegrated completely, ruby was inconclusive and cubic zirconia shattered, most likely from the thermal shock.

Shipboard Chromatography

All the samples for both RAS #9 & #10 were analyzed for H2 and CH4, and although no H2 was present, a temporally varying CH4 signal was detected with concentrations in the uM range. The Niskin bottles for the CTD casts further North along the ridge were also sampled for fluid, and the samples analyzed for methane. Methane was present in varying amounts, with a maximum close to 300 nM to the Northeast of Sasquatch.